|  |
| --- |
| **GACOFLEX® SF2036 WALKPAD****SOLVENT-FREE 100% SILICONE WALKWAY SYSTEM** |
| DESCRIPTION: | GacoFlex SF2036 WalkPad is a silicone-based, solvent-free, single-component waterproof elastomeric moisture-curing sealant combined with a reinforcing agent and is specifically formulated for exceptional durability.  |
| USAGE: | WalkPad is intended for application over GacoFlex Silicone Coatings and a variety of other roofing substrates to create a rooftop walkway for pedestrian maintenance traffic. Unlike conventional mats, WalkPad becomes an integral part of the roof. The yellow color provides a highly visible and aesthetic rooftop walkway, and when combined with GacoFlex WalkPad Granules will offer traction and resistance to wear under light foot traffic.  |
| COLOR: | Yellow |
| **APPLIED PRODUCT DATA** |
| WEATHERABILITY: | Excellent durability, color stability and chalk resistance.  |
| TOXICITY: | Not for use in contact with edible substances or potable water. |
| ADHESION: | Adhesion is excellent when applied directly over GacoFlex Silicone Coatings. A primer may be required for adhesion to other surfaces including built-up roofing, modified bitumen capsheet, single ply roofing (EPDM, TPO, PVC and Hypalon®), masonry, concrete, and wood. A primer must be used on all ferrous metals to prevent corrosion. Contact Gaco Western’s Technical Department for specific recommendations.  |
| **PRELIMINARY RESULTS BASED ON FILM THICKNESS OF 20 DRY MILS****Physical properties tests pending, in accordance with ASTM D-6694 with a film thickness of 60 dry mils.** |
| TENSILE: | ASTM D2370Initial tensile strength:Elongation:  | 306 ± 10 psi130% |
| TEAR RESISTANCE: | ASTM D624 Die C | 25 lbs per square inch |
| HARDNESS: | ASTM D2240 Shore A | 55  |
| WATER VAPOR PERMEANCE: | * ASTM E96 Procedure B
 | * 7.0 perms
 |
| LOW TEMPERATURE FLEX:  | * ASTM D522 Method B
 | * Pass
 |

|  |
| --- |
| **PACKAGED PRODUCT DATA** |
|  THEORETICAL COVERAGE: | 4 gallons per 100 sq. ft.NOTE: Actual coverage may be less due to surface profile, losses due to overspray and wind, and residual coating left in the container**.**  |
| SOLIDS:  | By Weight By Volume  | 96%95% |
| VOC: | 35 g/l |  |
| FLASH POINT:  | ASTM D3278  | 178°F (81°C) |
| STORAGE STABILITY: | Two years from date of manufacture when stored in sealed containers between 0°F - 80°F (-17°C - 26°C) |
| **APPLICATION** |
| MIXING: | Mix before application to ensure uniform color and consistency.  |
| THINNING: | Product is not intended to be thinned. |
| PRIMER:  | No primer is needed when WalkPad is being applied directly over GacoFlex Silicone Coatings. If applying WalkPad to any other surface, apply GacoFlex E5320 2-Part Epoxy Primer/Filler according to label directions. |
| APPLICATION: | Apply by brush or trowel as received. For application utilizing equipment contact Gaco Western. For cold weather application, keep material stored above 65°F (18°C). Do not apply if rain is expected within 1 hour. For application in temperatures below freezing or above 120°F (49°C) contact Gaco Western.* Apply WalkPad at a rate of 4 gallons per 100 sq. ft.
* When using WalkPad to create a rooftop walkway for pedestrian maintenance traffic, it is recommended that GacoFlex WalkPad Granules be applied to the wet product at a rate of 0.5 lb. per 100 sq.ft. to help ensure good traction. **CAUTION:** While the use of granules will improve traction, caution should still be exercised when walking on WalkPad, especially in wet conditions.

NOTE:  Application rate is job-specific. Additionalmaterial may be required due to surface profile, losses due to overspray and wind, and residual coating left in the container. |
| DRY TIME: | Allow to dry a minimum of 4 hours at 55°F (13°C) or higher, or until it can be safely walked on (product is moisture cure, low humidity will result in longer dry times).  |
| CLEAN UP: | Clean up application tools and equipment with GacoFlex Silicone Solvent. DO NOT USE WATER OR RECLAIMED SOLVENTS. |

For specific Safety and Health information please refer to Safety Data Sheet.